The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep126.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Chemical Resistant, Two Part Epoxy Features Glass Transition Temperature of +240°C

Widely used in the electronic, aerospace, optical and specialty OEM industries, Master Bond EP126 excels in high temperature applications up to +600°F. This two component product features unique handling properties as Part A is a moderate viscosity liquid and Part B is a powder. It can be easily mixed using a forgiving 100 to 50 ratio by weight. The mixed system is a malleable paste, with an exceedingly long open time of more than 5 days for a 100 gram batch. The curing is straightforward; 3-4 hours at 300°F or 2-3 hours at 350°F.

EP126 adheres well to many substrates including metals, composites, glass, ceramics, rubbers and many plastics. It offers a high tensile lap shear strength, tensile modulus and compressive strength of over 2,800 psi, 425,000-475,000 psi and 32,000-34,000 psi, respectively. This epoxy compound resists a variety of chemicals such as water, oils, acids, bases and many solvents. Additionally, it is formulated as a toughened system allowing it to withstand rigorous thermal cycling.

EP126 is dimensionally stable, has low shrinkage upon curing and is machineable. It also is a very good electrical insulator, especially as it retains high dielectric strength at elevated temperatures. When used as an adhesive and sealant, EP126 can be conveniently applied with a spatula or knife. This product has a service temperature range of -80°F to +600°F. EP126 features a shelf life of 6 months in its original, unopened containers and is available in kits ranging from ½ pints to 5 gallons.

Master Bond High Temperature Resistant Adhesives

Master Bond EP126 is a toughened, high temperature resistant epoxy with superior strength properties. This chemical resistant system has excellent electrical insulation properties. Read more about Master Bond’s high temperature resistant adhesives at http://www.masterbond.com/properties/high-temperature-resistant-bonding-sealing-and-coating-compounds or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep126

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #