The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep17htnd-ccm.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

One Component Glob Top Epoxy Meets NASA Low Outgassing Specifications

Master Bond EP17HTND-CCM is a new single component epoxy that is not premixed and frozen. It is more convenient to handle, apply and store than typical two component glob top systems. This black, heat curable compound has a flowable paste consistency ideal for glob top, chip coating and bonding applications. EP17HTND-CCM meets NASA low outgassing specifications and is serviceable from -80°F to +600°F [-62°C to +316°C]. This adhesive forms high strength bonds to a wide variety of similar/dissimilar substrates such as metals, ceramics, plastics, composites and various circuit board materials.

EP17HTND-CCM is thermally conductive and electrically non-conductive even upon exposure to hostile environmental conditions. EP17HTND-CCM has a high volume resistivity of more than 1015 ohm-cm at 75°F and over 1012 ohm-cm at 400°F. Its thermal conductivity is 9-10 BTU•in/ft2•hr•°F [1.4423 W/(m·K)] at 75°F. Also noteworthy is its ability to resist many chemicals including acids, bases, salts, fuels, oils and many solvents.

Formulated for various electronic applications, EP17HTND-CCM cures readily in 1-2 hours at 350°F [175°C] with a relatively low exotherm upon curing. It can be dispensed from a syringe, either manually or with an automatic dispenser. Master Bond EP17HTND-CCM is available for use in common size syringes ranging from 10 cc to 30 cc. For storage simple refrigeration at 40-45°F is recommended.

Master Bond High Temperature Resistant Adhesives

EP17HTND-CCM is a one part, heat cured epoxy that meets NASA low outgassing specifications. This high temperature resistant adhesive offers a great flow profile for glob top applications. Read more about Master Bond’s heat resistant adhesives at https://www.masterbond.com/properties/high-temperature-resistant-bonding-sealing-and-coating-compounds or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep17htnd-ccm

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #