The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep21ndcl.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Two Component Non-Drip Epoxy Paste Cures Optically Clear In Thin Sections

Master Bond EP21NDCL is a unique two component epoxy system that cures optically clear in thin sections, even though Part A is translucent and Part B is light amber. This non-drip compound is formulated for a variety of bonding, sealing and coating applications in the optical, opto-electronic, electrical, aerospace and specialty OEM industries.

EP21NDCL offers convenient handling with a one to one mix ratio by weight or volume. This ratio can be adjusted to deliver different properties. For example, a two to one mix ratio cures more rigid, while a one to two mix ratio produces a flexible system. EP21NDCL cures at room temperatures or more quickly at elevated temperatures.

Upon curing, this epoxy features durable bonds with high tensile lap shear, tensile and compressive strength of 2,600-2,800 psi, 6,500-7,500 psi and 12,000-13,000 psi, respectively. It bonds well to many substrates, such as metals, composites, glass, ceramics, rubbers and plastics, particularly acrylics and polycarbonates.

With a volume resistivity greater than 1014 ohm-cm, EP21NDCL offers impressive electrical insulation properties. It resists chemicals including water, oils, fuels, acids, bases and salts. This epoxy system also withstands rigorous thermal cycling over the wide service temperature range of -60°F to +250°F.

EP21NDCL has a shelf life of a year at 75°F in its original, unopened containers. It is available for use in container kits ranging in size from ½ pints to 5 gallons.

Master Bond Optically Clear Adhesives

Master Bond EP21NDCL is a two part, room temperature curing epoxy system with a paste consistency. It offers excellent electrical insulation, high physical strength properties and optically clarity. Read more about Master Bond’s optically clear adhesives at http://www.masterbond.com/properties/optically-clear-polymer-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep21ndcl

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #