-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep21tpfl-1ao

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Flexible, Two Component Epoxy Polysulfide System Features High Thermal Conductivity and Excellent Electrical Insulation Properties

Master Bond EP21TPFL-1AO is an electrically insulative, two part epoxy polysulfide system with a thermal conductivity of 9-10 BTU•in/ft2•hr•°F [1.30-1.44 W/(m·K)]. As a polysulfide based system, it has very good chemical resistance, particularly to fuels, oils, hydraulic fluids and related compounds. This unusual blend of properties, enables EP21TPFL-1AO to be a candidate for a variety of bonding, sealing, coating and encapsulation applications in the electronic, aerospace, specialty OEM and related industries.

With an elongation of 150-200%, EP21TPFL-1AO offers a high degree of flexibility and it can withstand intense thermal cycling and mechanical shock. This low viscosity system also has a hardness of 70-90 Shore A. The mix ratio is a forgiving two to three by weight or volume. Color coding facilitates mixing. Part A is black and Part B is off-white. Working life is a conveniently long 90-120 minutes at 75°F.

EP21TPFL-1AO fully cures at ambient temperatures and should not be heated. It has very good adhesion to metals, ceramics, composites, glass, and many rubbers and plastics. This compound is serviceable over the wide temperature range of -60°F to +250°F and has a 6 month shelf life in original, unopened containers. EP21TPFL-1AO is available for use in ½ pint, pint, quart, gallon or 5 gallon container kits.

Master Bond Polysulfide Adhesives

EP21TPFL-1AO is a low viscosity flexible epoxy polysulfide system that features reliable electrical insulation and thermal conductivity. Read more about Master Bond’s polysulfide adhesives at http://www.masterbond.com/products/polysulfide-adhesives-sealants-and-coatings or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep21tpfl-1ao

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #