-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep29lpao.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, Electrically Insulative Epoxy Features Long Working Life

Well suited for large potting and encapsulation applications, Master Bond EP29LPAO is a cost effective, two part system with a low viscosity, excellent flow properties and heat dissipation properties. Featuring convenient processing, this epoxy has a forgiving 100 to 50 mix ratio by weight and a pot life of 7-9 hours at room temperature for a 100 gram mass. Upon curing, EP29LPAO exhibits low exotherm, even in large volumes. This dimensionally stable formulation has low shrinkage upon cure, both linearly and volumetrically.

EP29LPAO delivers a thermal conductivity of 9-10 BTU•in/ft2•hr•°F [1.30-1.44 W/(m•K)] and superb electrical insulation values, including a volume resistivity exceeding 1015 ohm-cm. Additionally it offers an outstanding high strength profile, with a tensile modulus of 450,000-500,000 psi and a compressive strength of 24,000-26,000 psi at 75°F. This product bonds well to a wide range of substrates such as metals, glass, ceramics and many plastics. EP29LPAO cures at room temperature or more rapidly at elevated temperatures. An optimum cure schedule is overnight at 75°F followed by 4-5 hours at 150°F.

Often used in the aerospace, electronic, electrical and specialty OEM industries, EP29LPAO is serviceable from -60°F to +250°F. It resists chemicals including water, fuels and oils. This off-white colored system is available for use in ½ pint, pint, quart, gallon and 5 gallon container kits as well as premixed and frozen syringes.

Master Bond Low Exotherm Adhesives

EP29LPAO is a low viscosity epoxy system that features a long working life, reliable electrical insulation and low exotherm suitable for large potting and encapsulation applications. Read more about Master Bond’s low exotherm adhesives at http://www.masterbond.com/properties/low-exothermic-epoxy-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep29lpao

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #