The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep29lptcht.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Underfill Epoxy Offers Thermal Conductivity and Electrical Insulation

Master Bond EP29LPTCHT is a two component, low viscosity epoxy compound that can be effectively utilized for underfill and encapsulation applications. It does not need excessive heat for curing and has a long working life at room temperature. This system is electrically insulative and thermally conductive with very fine particle size filler material. EP29LPTCHT can be easily dispensed into tiny gaps and when used as an adhesive, it forms thin bond lines from 5 to 15 microns, resulting in a significantly low thermal resistance of 12-15 x 10-6 K•m2/W.

EP29LPTCHT features excellent flow properties with an initial mixed viscosity of 5,000-15,000 cps. It offers a long working life after mixing, for example a 100 gram batch at 75°F will yield an open time of 10-12 hours. EP29LPTCHT has a thermal conductivity of 9-10 BTU•in/(ft2•hr•°F) and a volume resistivity of more than 1015 ohm-cm, both measured at 75°F.

The recommended cure schedule is overnight at room temperature followed by 4-5 hours at 160°-180°F. This noteworthy processing characteristic makes it ideal for substrates which are heat sensitive. After curing EP29LPTCHT features an exceptionally low coefficient of thermal expansion of 22-24 x 10-6 in/in/°C along with a compressive strength of 24,000-26,000 psi and a hardness of 80-90 Shore D. It is available in premixed and frozen syringes, 1/2 pint kits, pint kits, and quart kits. The color of Part A is off white and the color of Part B is white.

Master Bond Epoxies for Underfill Applications

Master Bond EP29LPTCHT is a two component, low viscosity, thixotropic epoxy ideal for underfill applications that require thermal conductivity and electrical insulation. This dimensionally stable compound offers a low coefficient of thermal expansion and high compressive strength properties. Read more about Master Bond’s underfill compounds at https://www.masterbond.com/industries/underfill-encapsulants or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep29lptcht

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #