The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep30ng

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Graphene Filled Epoxy Offers 5.5 W/(m•K) Thermal Conductivity

Master Bond EP30NG is a two part epoxy adhesive system developed for applications that require high thermal conductivity. It contains a specialty graphene filler which contributes not only to its high compressive strength, but also to its enhanced dimensional stability. EP30NG achieves an extraordinary thermal conductivity of 38.15 BTU•in/(ft2•hr•°F) [5.5 W/(m•K)] at room temperature while its compressive strength measures 22,000-24,000 psi upon cure. It has a low coefficient of thermal expansion of 24-26 x 10-6 in/in/°C and exhibits a Shore D hardness of 85-95.

According to Rohit Ramnath, Senior Product Engineer, "EP30NG is ideal for bonding applications where some contact pressure can be applied. The minimum bond line thickness is 0.18mm, since graphene nanoparticles tend to agglomerate to form larger particles." This epoxy system is formulated to cure at room temperature or more rapidly at elevated temperatures. Part A has a thick paste consistency and Part B is a low viscosity liquid.

EP30NG bonds well to a variety of substrates including metals, composites, ceramics, glass and many plastics. The service temperature range is -60°F to +300°F. The product is available in 30 cc jar kits, 1/2 pint kits, and pint kits.

Master Bond Thermally Conductive Adhesives

Master Bond EP30NG is a thermally conductive epoxy system containing graphene filler. It is suitable for applications where high thermal conductivity is needed and the small amount of electrical conductivity is not a factor. Read more about Master Bond’s thermally conductive adhesives at https://www.masterbond.com/properties/thermally-conductive-epoxy-adhesives or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/newsrelease/ep30ng

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #