The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep30ns .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Nanosilica Filled Epoxy with High Abrasion Resistance Meets NASA Low Outgassing Specifications

Master Bond EP30NS is a two component epoxy system that cures at room temperature or more rapidly at elevated temperatures. It is optically clear especially in thin sections and can be used as an adhesive, sealant, coating and encapsulation compound. EP30NS offers dimensional stability, linear shrinkage of less than 0.01%, excellent physical strength characteristics and cures rigid. Most significantly, this epoxy system has been independently tested per ASTM D4060-14 for abrasion resistance for 1,000 cycles and exhibited a loss of weight of only 18.3 mg. This value exceeds typical epoxy compositions and demonstrates the compound’s ability to withstand exposure to scuffing, gouging, scraping, scratching and wear.

“Master Bond EP30NS has a Shore D hardness of 80-90”, says Rohit Ramnath, Senior Product Engineer. “It possesses a coefficient of thermal expansion of 30-35 x 10-6 in/in/°C and is well suited for small potting applications. Its long term electrical insulation characteristics are quite impressive. Also noteworthy is that EP30NS has a tensile strength of 9,000-11,000 psi and a refractive index of around 1.56 at 589 nm.”

This formulation has a 4 to 1 mix ratio by weight. Working life after mixing a 100 gram batch is 20-30 minutes at 75°F. It has a mixed viscosity of 25,000-45,000 cps and flows readily. This system is available for use in ounce, ½ pint, pint, quart and gallon kits. It can also be purchased in double barrel cartridges. These cartridge containers can be dispensed using gun applicators.

Master Bond Abrasion Resistant Adhesives

Master Bond EP30NS is a rigid, optically clear, nanosilica filled epoxy system that features outstanding resistance to wear, chemical exposure and moisture. This product has high dimensional stability and outstanding dielectric properties. Read more about Master Bond’s abrasion resistant adhesives at https://www.masterbond.com/properties/abrasion-resistant-adhesives-and-coatings or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep30ns

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #