-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep3hts-tc .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Highly Thermally Conductive, NASA Low Outgassing Silver Filled Epoxy

Master Bond EP3HTS-TC is a one part, NASA low outgassing rated epoxy, with an outstanding thermal conductivity of 16-17 W/(m·K). It cures rapidly at temperatures of around 250-300°F [~ 125-150°C], and has an unlimited working life at room temperature. The material features a thixotropic paste consistency and is not pre-mixed and frozen. It is well suited for automatic dispensing equipment or manual syringes and can be applied without any tailing. Primarily, it is formulated for use as a die attach and special purpose bonding material.

“EP3HTS-TC utilizes a non-sintering silver technology to provide ultra high heat transfer capability.” says Rohit Ramnath, Senior Product Engineer. “It is designed without compromise to dispensability or adhesion strength, while maximizing performance properties.” EP3HTS-TC is highly electrically conductive, with a volume resistivity of less than 1x10-6 ohm-cm.

The system exhibits good dimensional stability, resists thermal cycling, and has a low coefficient of thermal expansion of 20-23 x 10-6 in/in/°C. Die shear strength is 9-12 kg-f at 75°F for a 2 x 2 mm [80 x 80 mil] area. It has a glass transition temperature of 58°C and is serviceable over the temperature range of -80°F to +400°F. This compound adheres well to a variety of substrates such as metals, composites, glass, ceramics, semiconductor materials and many plastics. Packaging is available in syringes, 20, 50 and 100 gram jars, as well as single and multiple pound containers.

Master Bond Thermally Conductive, NASA Low Outgassing Systems

Master Bond EP3HTS-TC is a one part epoxy system with a paste consistency for die attach and bonding applications. It meets NASA low outgassing requirements and has ultra high thermal conductivity.  Read more about Master Bond’s NASA low outgassing adhesives at https://www.masterbond.com/certifications/nasa-low-outgassing or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep3hts-tc

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #