-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep40nd .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened, Non-Drip Epoxy Meets NASA Low Outgassing Specifications

Master Bond EP40ND is a two component epoxy system, designed for bonding, sealing and coating applications. It is a non-drip, toughened system with an easy to use 1:1 mix ratio by weight or volume. EP40ND meets NASA low outgassing specifications and has a high elongation of 80-90% at 75°F. It adheres well to many plastics, such as polycarbonates and acrylics, making it appropriate for applications that use substrates prone to stress cracking.

This flexible system provides a low tensile modulus of 1,000-1,500 psi, and a relatively high lap shear strength of 1,600-1,800 psi. EP40ND has a Shore D Hardness measuring between 50-60 at 75°F. Serviceable from -100°F to +250°F, this electrically insulative compound can withstand rigorous thermal cycling, vibration, impact and shock.

EP40ND cures within 2-3 days at room temperature, or faster with the addition of heat. The viscosity of Part A is 50,000-100,000 cps, Part B is a thixotropic paste. It has a long working life after mixing. In addition to plastics, this epoxy adheres well to a variety of dissimilar substrates such as metals, composites, glass, and ceramics. EP40ND can be used in aerospace, semiconductor, electronic, opto-electronic and medical device industries. It is available in standard packaging, as well as premixed and frozen syringes. It is also available in double barrel cartridges for use with a gun dispenser.

Master Bond Flexibilized and Toughened Adhesives

Master Bond EP40ND is a high strength two part epoxy with superior elongation and toughness. It meets NASA low outgassing requirements and can be used for bonding, sealing and coating applications. Read more about Master Bond’s flexibilized and toughened adhesives at https://www.masterbond.com/properties/flexibilized-and-toughened-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep40nd

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #