The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep46ht-1ao.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Two Component, Thermally Conductive Epoxy Resists High Temperatures

Formulated for bonding and sealing applications, Master Bond EP46HT-1AO is widely used in the aerospace, electronic and specialty OEM industries. Unlike most conventional two component epoxies, EP46HT-1AO cures with the addition of heat, which allows it to have a working life exceeding 24 hours. It has a forgiving 100 to 30 mix ratio by weight and bonds well to metals, composites, glass, ceramics and many plastics.

EP46HT-1AO combines thermal conductivity and electrical insulation properties. This dimensionally stable system provides a tensile strength over 7,500 psi, a compressive strength of 26,000 psi and a tensile lap shear strength greater than 1,500 psi at room temperature. EP46HT-1AO also withstands a variety of chemicals including oils, water, acids, bases and solvents.

This unique compound is serviceable over the temperature range of -73°C to +288°C (-100°F to +550°F) and offers a glass transition temperature of 215°C. It should be noted that EP46HT-1AO is relatively exothermic and should not be cured in sections greater than 20-30 thousandths of an inch thick and a bondline thickness is typically 2-7 thousandths of an inch.

This epoxy is available in ½ pint, pint, quart, gallon and 5 gallon container kits. Part A of this system is tan in color and Part B is moderately dark brown. EP46HT-1AO has a 6 month shelf life at ambient temperatures in original, unopened containers.

Master Bond Thermally Stable Adhesives

Master Bond EP46HT-1AO is thermally conductive and electrically insulative for bonding and sealing applications. This high strength, two component epoxy withstands temperatures up to +550°F. Read more about Master Bond’s heat resistant adhesives at http://www.masterbond.com/properties/high-temperature-resistant-bonding-sealing-and-coating-compounds or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep46ht-1ao

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #