The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep46ht-2ao-black.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Thermally Conductive, High Temperature Resistant Epoxy Passes NASA Low Outgassing Tests

Certified to meet ASTM E595 NASA low outgassing standards, Master Bond EP46HT-2AO Black is well suited for the aerospace, electronic, opto-electronic industries and can be used vacuum environments. This two component system blends thermal stability with a high strength profile for a variety of bonding, sealing and encapsulation applications.

EP46HT-2AO Black combines superior thermal conductivity of 9-10 BTU•in/ft2•hr•°F [1.2981-1.4423 W/(m·K)] and reliable electrical insulation with a volume resistivity exceeding 1014 ohm-cm at room temperature. It has a glass transition temperature of 200-210°C and is serviceable over the wide temperature range of -100°F to +500°F [-73°C to +260°C]. This dimensionally stable system delivers a tensile strength of 6,000-7,000 psi, compressive strength of 26,000-28,000 psi and tensile lap shear strength of 1,400-1,600 psi at 75°F. EP46HT-2AO Black also withstands a variety of chemicals including oils, water, acids, bases and fuels.

Unlike most traditional two part epoxies, EP46HT-2AO Black cures with the addition of heat, which allows it to have a working life of over 24 hours. It has a forgiving 100 to 30-35 mix ratio by weight and upon mixing, this thixotropic system has a viscosity of 140,000-280,000 cps. It bonds well to metals, composites, glass, ceramics, rubbers and many plastics.

This epoxy is available in ½ pint, pint, quart, gallon and 5 gallon container kits. Part A of this system is black in color and Part B is gray. EP46HT-2AO Black has a minimum 6 month, maximum 1 year shelf life at ambient temperatures in original, unopened containers.

Master Bond Thermally Stable Adhesives

Master Bond EP46HT-2AO Black is thermally conductive and electrically insulative adhesive, sealant and potting compound that meets NASA low outgassing requirements. This high strength, two component epoxy withstands temperatures up to +500°F. Read more about Master Bond’s heat resistant adhesives at http://www.masterbond.com/properties/high-temperature-resistant-bonding-sealing-and-coating-compounds or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep46ht-2ao-black

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #