The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep48tc.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Two Component Epoxy with Ultra Low Thermal Resistance and Superior Electrical Insulation Properties

Featuring special high thermal conductive fillers, Master Bond EP48TC is two part epoxy paste that can be applied in bond lines as thin as 10-15 microns. This material offers exceptionally low thermal resistance of 5-7 x 10-6 K•m2/W, which imparts impressive heat transfer capabilities and thermal conductivity of 20-25 BTU•in/ft2•hr•°F [2.88-3.60 W/(m·K)]. It can be used in applications in the aerospace, electronic, optical, specialty OEM and many other high-tech industries.

EP48TC has a tensile lap shear strength ranging from 900-1,100 psi and bonds well to a wide variety of substrates, including metals, composites, glass, ceramics and many plastics. Even in thin sections, its strength retention is outstanding. It also has a low coefficient of thermal expansion, low shrinkage upon curing and excellent dimensional stability.

EP48TC has a forgiving 100 to 40 mix ratio by weight, or 100 to 50 mix ratio by volume. The working life for a 100 gram batch at 75°F is 90-120 minutes. The epoxy cures at room temperature or more quickly at elevated temperatures. It is serviceable over the temperature range of -100°F to +300°F. The color of Parts A and B is gray. EP48TC is available in standard packaging ranging from ½ pint to 5 gallon container kits.

Master Bond Adhesives for Heat Dissipation Applications

Master Bond EP48TC is a two component epoxy with high thermal conductivity that can be applied in very thin sections. Read more about Master Bond’s liquid thermal interface materials at http://www.masterbond.com/properties/thermally-conductive-epoxy-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep48tc

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #