The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep62-1lpspmed .

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Ultra Low Viscosity Biocompatible Epoxy for Medical Electronic Applications

Formulated for medical electronic applications, Master Bond EP62-1LPSPMed is a biocompatible two part epoxy that has a mixed viscosity of 150-300 cps. Its ultra low viscosity makes it ideal for use in underfill, impregnation and porosity sealing applications, while it also performs well in bonding, coating or encapsulation. This product exhibits excellent wetting properties and can readily flow by capillary action in tight clearances or beneath devices. It adheres well to metals, plastics, composites, polyimides, glass and ceramic substrates.

EP62-1LPSPMed has an advantageously long working life of 12-24 hours for a 100 gram mass and requires moderate heat for curing. Cure schedule is overnight at room temperature followed by 60-90 minutes at 80-100°C. The higher the temperature the faster the cure. Post curing at 100-150°C for 3-4 hours will optimize its properties.

Master Bond EP62-1LPSPMed passes USP Class VI and ISO 10993-5 cytotoxicity requirements. It also has been tested for 1,000 hours at 85°C/85% RH. It has excellent toughness, tensile strength of 11,000-12,000 psi and resists repeated cycles of ethylene oxide, radiation, and chemical sterilization. This compound has volume resistivity of more than 1014 ohm-cm, withstands mechanical shock/vibration and is serviceable from 4K to +400°F. In very thin sections it will transmit light, but in thicker sections it is opaque. Shore D hardness is 75-85 and its glass transition temperature is 125-130°C.

EP62-1LPSPMed has a 100 to 25 mix ratio by weight and can be supplied in standard sized units: ½ pint, pint, quart, gallon, 5 gallon kits. It can also be packaged in premixed and frozen syringes, as well as in cartridges for gun dispensers. Shelf life in original unopened containers is 6 months.

Master Bond Biocompatible Adhesives

Master Bond EP62-1LPSPMed is a tough, thermally stable, high strength, low viscosity epoxy that meets USP Class VI and ISO 10993-5 specifications. This two part system can withstand exposure to repeated sterilization and withstand thermal cycling, mechanical vibration. Read about Master Bond medical grade adhesives at https://www.masterbond.com/properties/biocompatible-adhesives or contact technical support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/ep62-1lpspmed

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #