The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/ep62-1lpsp.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Optically Clear, Low Viscosity Epoxy Features a Long Open Time at Room Temperature

Master Bond EP62-1LPSP delivers an array of strength, electrical and handling properties that are well suited for bonding, sealing, coating and encapsulation applications. With a tensile lap shear strength exceeding 2,000 psi, it bonds well to a variety of substrates including metals, composites, glass and many plastics.

This optically clear epoxy has a non-critical four to one mix ratio by weight and features an open time of 12-24 hours at ambient temperatures. EP62-1LPSP has a thin mixed viscosity of 150-300 cps, which can be further lowered by adding heat. Its low exotherm while curing allows it to be used for large encapsulations. It offers a variety of cure schedules and can be cured at temperatures as low as 60-70°C. Faster cures can be achieved at 125°C.

Featuring a glass transition temperature of greater than 125°C, EP62-1LPSP is a thermally stable system that is serviceable over the wide temperature range of -60°F to +400°F. It withstands exposure to chemicals such as water, fuels, oils, solvents, acids and bases. EP62-1LPSP is a reliable electrical insulator and has a volume resistivity over 1014 ohm-cm. This blend of high performance properties allows this product to be used in aerospace, electronic, fiber-optic, optoelectronic and specialty OEM applications.

EP62-1LPSP is available for use in standard ½ pint, pint, quart, gallon and 5 gallon kit containers. It can be applied by brush, paint roller, syringe or gun dispenser.

Master Bond Low Viscosity Adhesives

Master Bond EP62-1LPSP is high temperature resistant, two part epoxy with an ultra low viscosity. This optically clear system also provides high tensile and tensile lap shear strength. Read more about Master Bond’s low viscosity adhesives at http://www.masterbond.com/properties/low-viscosity-adhesives-sealants-and-coatings or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep62-1lpsp

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #