-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/ep77m-fmed.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Fast Curing, Silver Filled Epoxy Meets ISO 10993-5 Cytotoxicity Standards

Master Bond EP77M-FMed is a two part epoxy adhesive and sealant designed for use in the assembly of medical devices. It meets the ISO 10993-5 requirements and is not considered to have a cytotoxic effect. “This product has been formulated to provide excellent electrical and thermal conductivity properties, while keeping in mind processing constraints for heat sensitive components in sensors used for medical devices or wearable electronics,” says Rohit Ramnath, Senior Product Engineer.

As a silver filled system, EP77M-FMed provides excellent electrical conductivity, with a low volume resistivity of 10-3 ohm-cm.  It provides a thermal conductivity of 1.44-1.73 W/(m•K), resists thermal cycling and has a Shore D hardness of 40-50 at room temperature. It can withstand exposure to water, liquid sterilants, anti-microbial disinfectants and EtO sterilization. It offers a tensile strength of 2,000-3,000 psi and a tensile modulus of 250,000-300,000 psi at 75°F. This system is serviceable over the temperature range of -100°F to +250°F.

EP77M-FMed has an easy to use one to one mix ratio by weight or volume and is fast setting, especially when compared to other silver filled systems. It sets up in 15-20 minutes at 75°F and fully cures at room temperature in 24 hours. This compound has a flowable paste like consistency and bonds well to a variety of substrates including metals, glass, ceramics, rubbers and many plastics. It is packaged in 20 gram, 50 gram, 100 gram, one pound and multiple pound cans. The color of Parts A and B is silver. EP77M-FMed does not contain any solvents and is RoHS compliant.

Master Bond Biocompatible Epoxy Systems

Master Bond EP77M-FMed is a two component epoxy that passes ISO 10993-5 specifications for cytotoxicity.  Typically, medical grade adhesives, sealants, coatings and potting/encapsulation compounds need to be non-cytotoxic and show compatibility with blood and body fluids. Read more about Master Bond’s biocompatible adhesives at https://www.masterbond.com/properties/biocompatible-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/ep77m-fmed

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #