-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/super-gel-9ao.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Dimensionally Stable Two Component Urethane Modified Epoxy Gel Is Thermally Conductive

Primarily used for potting and encapsulation applications, Master Bond Super Gel 9AO is a  soft, urethane modified gel-like epoxy that offers thermal conductivity and electrical insulation properties. This two part system is also employed for bonding and sealing as it adheres well to a variety of substrates including metals, glass, ceramics and many rubbers and plastics.

With a low hardness of 20-30 Shore A, Super Gel 9AO is able to encapsulated sensitive electronic components. Expensive parts are retrievable by cutting the compound with a sharp knife or razor blade. This process can be conducted without the compound shattering. This softness allows it to withstand thermal cycling as well as thermal and mechanical shock. It is serviceable from -100°F to +200°F and resists chemicals such as water, oils and fuels.

Super Gel 9AO has a 2 to 1 mix ratio by weight or volume and has a low to moderate viscosity. This system offers a working life of 6-8 hours at room temperature, depending on the quantity that is mixed. It cures at room temperature with little exotherm, enabling it to be cast several inches thick.

This light gray colored system is available for use in standard packaging from ½ pints to 5 gallon container kits and in specialty packaging with gun dispensers and syringes. Super Gel9AO is currently used in the aerospace, electronic, optical, electro-optical and other specialty industries.

Master Bond Dimensionally Stable Adhesives

Master Bond Super Gel 9AO is a thermally conductive system for potting, encapsulation, bonding and sealing applications. Despite its low durometer, this two component, urethane modified gel-like epoxy is dimensionally stable. Learn more about our dimensionally stable adhesives at http://www.masterbond.com/properties/dimensionally-stable-epoxy-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/super-gel-9ao

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #