-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/supreme-10htf-1

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened, One Component Epoxy Features High Bond Strength and Cryogenic Serviceability

Combining simple handling properties with high strength, Master Bond Supreme 10HTF-1 is a single part adhesive/sealant for a variety of applications in the aerospace, electronic, optical, specialty OEM and related industries. At room temperature, this smooth paste system has an “unlimited” working life and cures rapidly at elevated temperatures. For example, typical cure schedules for Supreme 10HTF-1 are 5-10 minutes at 300°F or 15-20 minutes at 250°F.

Supreme 10HTF-1 delivers impressive physical strength values for tensile lap shear, tensile and T-peel of >3,200 psi, 6,500-7,500 psi and 20-25 pli, respectively. This system bonds well to a wide variety of substrates including metals, composites, glass, ceramics, rubbers and many plastics. It has very low shrinkage upon curing, is dimensionally stable and has a Shore D hardness >70. As a toughened system, Supreme 10 HTF-1 is capable of withstanding rigorous thermal cycling as well as mechanical shock and vibration.

Supreme 10HTF-1 offers cryogenic serviceability over the wide temperature range of 4K to +400°F. The adhesive resists an array of chemicals such as water, fuels, acids, bases and many solvents. Also, it is a reliable electrical insulator. Volume resistivity is 1013 ohm-cm.

This compound is gray, but other colors are available. Supreme 10HTF-1 is available in standard packaging ranging from ½ pint to 5 gallon containers as well as specialty packaging including cartridges and syringes.

Master Bond Flexible and Toughened Adhesives

Supreme 10HTF-1 is a high strength, toughened system that cures quickly at elevated temperatures. Read more about Master Bond’s flexible/toughened adhesive systems at http://www.masterbond.com/properties/flexibilized-and-toughened-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/supreme-10htf-1

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #