-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

A high resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at https://www.masterbond.com/newsrelease/supreme-11aohtmed.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Two Part Structural Epoxy Meets ISO 10993-5 for Non-Cytotoxicity

Master Bond Supreme 11AOHTMed is a two component epoxy featuring thermal conductivity and electrical insulation. This system fully passes ISO 10993-5 testing for non-cytotoxicity and is recommended for bonding and sealing in medical device applications.

Supreme 11AOHTMed has reliable electrical insulation properties with a volume resistivity exceeding 1014 ohm-cm at 75°F. It also exhibits thermal conductivity of around 4 to 5 BTU·in/ft²·hr·°F (0.58-0.72 W/m/K). The system provides high bond strength properties with a lap shear strength of 3,200-3,400 psi, a tensile strength of 7,000-8,000 psi and a compressive strength of 20,000-22,000 psi. This toughened formulation is designed to withstand thermal cycling and offers a wide service temperature range from -112°F to +400°F (-80°C to 204°C).

Supreme 11AOHTMed cures at room temperature in 24-36 hours, and faster with heat, in 1-2 hours at 200°F. To optimize properties, the recommended cure schedule is overnight at room temperature, followed by a post cure at 120-150°F for 2-3 hours or preferably longer. It bonds well to a wide variety of substrates including metals, ceramics, glass, rubbers, and many plastics. This epoxy system has a convenient 1:1 mix ratio by weight, with the mixed material being a thixotropic paste. To eliminate the need for manual measuring and mixing, it can be packaged in double barrel cartridges for gun kits. It is also available in standard jars and cans, ranging in size from ½ pint to gallon containers.

Master Bond Adhesives for Medical Device Manufacturing

Supreme 11AOHTMed is a thermally conductive, electrically isolating epoxy offering high strength and a wide service temperature range. This two component epoxy passes ISO 10993-5 certification for non-cytotoxicity and is well suited for a variety of bonding and sealing applications in medical device assembly. Read more about Master Bond’s biocompatible systems for medical devices at https://www.masterbond.com/properties/biocompatible-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: https://www.masterbond.com/tds/supreme-11aohtmed.

Check out new videos on our YouTube channel: https://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #

-----------------------------------------------------------------