The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/supreme-34ca.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Heat Curable Corrosion Resistant Epoxy System Withstands Temperatures up to 500°F

Master Bond Supreme 34CA is a high strength structural epoxy adhesive featuring superior resistance to aggressive chemicals such as acids, bases, solvents and oils. Serviceable from -80°F to +500°F this solvent free formulation has a working life of more than 24 hours per 100 gram batch at room temperature. It has good flow properties, a mixed viscosity of 7,000-20,000 cps, a mix ratio of 100 to 50 by weight and cures upon exposure to heat. This product can be dispensed manually or via automated dispensing systems.

“This unique compound offers outstanding long term durability. It adheres well to both similar and dissimilar substrates such as metals, glass, ceramics and plastics,” said Rohit Ramnath, senior product engineer. “It can be used to replace traditional mechanical fastening techniques in applications requiring high temperature and chemical resistance.”

Master Bond Supreme 34CA has a tensile lap shear strength >2,500 psi and a tensile strength >12,000 psi. This electrically insulative epoxy has a volume resistivity of >1014 ohm-cm. It also features a Tg of 200-210°C and a Shore D hardness of >75.

The color of Part A is black and Part B is amber. It is available for use in ½ pint, pint, quart, gallon, 5 gallon pail kits and in gun applicators. Supreme 34CA can be used as a corrosion resistant coating, as well as for bonding, sealing and filament winding applications.

Master Bond Structural Adhesives

Master Bond Supreme 34CA is a high temperature resistant epoxy adhesive with outstanding chemical resistance characteristics. This two component , electrically insulative, high strength adhesive has a long working life after mixing. Read more about our structural adhesives at https://www.masterbond.com/applications/structural-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/supreme-34ca

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #