The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/supreme-45htq-4.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Toughened, High Strength, Two Component Epoxy Offers Chemical, Abrasion and High Temperature Resistance

Featuring a silicon carbide filler, Master Bond Supreme 45HTQ-4 is a toughened epoxy for high performance bonding, sealing, coating and casting. This specialty system can be used for a wide variety of special industrial, aerospace, OEM and oil processing applications, especially in downhole situations.

Supreme 45HTQ-4 has the unique combination of exceptional chemical, temperature and abrasion resistance. Serviceable from -100°F to +450°F, it is capable of withstanding rigorous thermal cycling. This compound offers high tensile lap shear, compressive and tensile strength of 1,400-1,600 psi, 24,000-26,000 psi and 8,000-9,000 psi, respectively. Supreme 45HTQ-4 also retains its strength at elevated temperatures. It is a dimensionally stable system with low shrinkage upon curing. Additionally, this epoxy has excellent electrical insulation properties with a dielectric constant at 60 Hz of 4.6 and a volume resistivity exceeding 1014 ohm-cm.

Supreme 45HTQ-4 has a mix ratio of 100 to 30 by weight and a thixotropic paste consistency. It features a long pot life of more than 12 hours at room temperature for a 100 gram batch. This compound requires oven curing at 250-300°F with various cure schedules. A post cure of 4 hours at 350°F will optimize properties. Bond strength to a wide variety of substrates, including metals, composites, ceramics, rubbers and most plastics is excellent.

This gray colored system is available for use in standard packaging options ranging from ½ pint to 5 gallon kits as well as specialty Semkits. Supreme 45HTQ-4 has a shelf life of 6 months at ambient temperatures.

Master Bond Abrasion Resistant Adhesives

Supreme 45HTQ-4 is a toughened, silicon carbide filled epoxy system that withstands wear, chemicals and high temperatures. Read more about Master Bond’s abrasion resistant adhesives at http://www.masterbond.com/properties/abrasion-resistant-adhesives-and-coatings or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/supreme-45htq-4

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #