-----------------------------------------------------------------

The following is a news release from Master Bond Inc. You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution version of this image and files with the body text of this release in Word, HTML and text formats are available at http://www.masterbond.com/newsrelease/uv15x-6nm-2.

-----------------------------------------------------------------

## FOR IMMEDIATE RELEASE

Non-Yellowing UV Curable System Has Superior Abrasion Resistance

Master Bond UV15X-6NM-2 is a one component UV curing urethane acrylate system formulated for a variety of bonding, sealing, coating and encapsulation applications. This moderate viscosity product features flexibility, toughness and abrasion resistance. It is widely used for fiber-optic, optical, electronic, semiconductor, microelectronic and laser applications.

UV15X-6NM-2 features an elongation exceeding 200%, which contributes to its ability to withstand rigorous thermal cycling and mechanical shocks. It is serviceable over the wide temperature range of -80°F to +250°F. It also has very good chemical resistance, especially to water, cleaning agents and oils. With a refractive index of 1.50, this compound is optically clear and has impressive non-yellowing properties.

This special formulation cures readily in 10-30 seconds when exposed to a UV light source. The rate of cure depends upon the system’s distance from the light source, the thickness of the section and the intensity of the light source. It is not oxygen inhibited. Cures can be obtained in sections approaching 1/4 inch thick. As a reliable electrical and thermal insulator, UV15X-6NM-2 is well suited for potting and encapsulation. It also bonds well to a variety of substrates including glass, plastics including polycarbonates and acrylics, composites, metals and many types of rubbers.

UV15X-6NM-2 is available for use in standard packaging options from ½ pints to 5 gallons. For easy dispensing, this product can be purchased in 3 cc to 60 cc syringe applicators.

Master Bond Optically Clear Adhesives

Master Bond UV15X-6NM-2 is an optically clear UV curable system for bonding, sealing, coating and potting applications that require non-yellowing properties, toughness and abrasion resistance. Read more at http://www.masterbond.com/properties/optically-clear-polymer-adhesives or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Note to Editors:

For a full product description, please visit: http://www.masterbond.com/tds/uv15x-6nm-2

Check out new videos on our YouTube channel: http://www.youtube.com/user/MasterBondVideo

You can embed any of our videos on your website.

CONTACT

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: +1-201-343-8983

Fax: +1-201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ 07601-3922

Web: www.masterbond.com

# # #