This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep17ht-3.

----------------------------------

FOR IMMEDIATE RELEASE

Single Component Snap Cure Epoxy Has Outstanding 
Electrical Properties and Chemical Resistance

HACKENSACK, NJ – May 6, 2010 – Master Bond EP17HT-3 is a one part epoxy that sets up in 20 to 30 seconds and snap cures in only 2 to 3 minutes at 250°F–300ºF. As a one part system, no mixing is required and the epoxy can be cured in sections up to 1/4” thick. Moreover, its working life is indefinite as it will not gel until heated above 200ºF.

With a volume resistivity of greater than 1014 ohm-cm, EP17HT-3 has excellent electrical insulation and chemical resistance characteristics. It is resistant to a wide range of chemicals including water, oil and most organic solvents. Other typical features include a Shore D hardness that exceeds 85 and a tensile lap shear of 2100 psi.

Master Bond’s EP17HT-3 adhesive has superior temperature resistance with a service operating temperature range of -60ºF to +400ºF. It is 100% reactive and contains no solvents or diluents. It is also available in a paste version called EP17HT-3ND and a slightly toughened variant called Supreme 17HT-3 which is ideal for bonding dissimilar substrates and applications subject to thermal cycling. Each product comes in half pints, pints, quarts, gallons and 5 gallon container sizes.

Master Bond’s EP17HT-3 one part snap curing epoxy features high temperature resistance and has outstanding electrical properties and chemical resistance. Read more about Master Bond’s one part epoxy formulations at http://www.masterbond.com/lp/tabs/tp_byt_1ptepoxy.html, or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #