This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep31.

----------------------------------

FOR IMMEDIATE RELEASE

New Chemically Resistant Electrically

Insulative Structural Adhesive

with Exceptional Strength Properties

HACKENSACK, NJ – July 20, 2010 – For superb adherence to a wide variety of substrates including many metals, plastics, rubbers, ceramics and glass, Polymer System EP31 was developed by Master Bond Inc.  This two part system features extraordinary adhesion with a lap shear strength exceeding 4,600 psi, a peel strength surpassing 40 pli, a tensile modulus of more than 410,000 psi and a flexural strength of over 13,000 psi.

With an excellent resistance to many chemicals including water, oil and fuels, it is also an outstanding electrical insulator.  EP31 has a versatile cure schedule and can cure at room temperature or more quickly at elevated temperatures.

Other notable characteristics include a Shore D Hardness of greater than 75 and low shrinkage upon cure.  It is easily processed with a convenient 3 to 1 mix ratio by weight and has a service temperature range of -60ºF to 250ºF.

Available in both black and optically clear, EP31 is sold in half pints, pints, quarts, 1 gallon and 5 gallon containers.  It is also available in a convenient non-drip version called EP31ND.

Master Bond’s Two Part Epoxies

Master Bond’s EP31 is a versatile, two component epoxy system for demanding structural applications.  Read more about Master Bond’s two part epoxy formulations at http://www.masterbond.com/lp/tabs/tp_byt_2ptepoxy.html, or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #