This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ep42ht-2nd2med-black.

----------------------------------

FOR IMMEDIATE RELEASE

Medical Grade Epoxy Adhesive Withstands 
High Temperatures and Repeated Sterilization

HACKENSACK, NJ – July 14, 2011 – Capable of tolerating the harsh environments of the medical industry, Master Bond EP42HT-2ND2MED (Black) fully complies with the testing requirements of USP Class VI plastics. This two component epoxy resists recurrent autoclaving and sterilizations including radiation, steam, ethylene oxide, and chemical sterilants.

EP42HT-2ND2MED (Black) is an excellent electrical insulator with a volume resistivity over 1012 ohm-cm, a thermal expansion coefficient of 35 to 40 in/in x 10-6/°C, a dielectric constant of 3.8, and a tensile strength exceeding 12,000 psi at ambient temperatures. Heat resistant up to 450°F, it also withstands chemicals such as inorganic and organic acids, alkalis, organic solvents, and aromatic hydrocarbons.

This epoxy conveniently cures at room temperature in 48 to 72 hours. Its optimal curing schedule is overnight at room temperature followed by 2 to 3 hours of heat curing at 100°C to 125°C. EP42HT-2ND2MED (Black) has a noncritical mix ratio of 100:40 by weight or 100:50 by volume, and a paste consistency with minimal flow when applied. It offers a lengthy working life of 30 to 45 minutes for a mixed 100 gram batch at ambient temperatures, which can be increased by using shallow mixing vessels or mixing smaller batches. Parts A and B for EP42HT-2ND2MED (Black) are available for use in syringes, half pints, pints, quarts, gallons, and five gallon containers.

Master Bond Medical Adhesives

Medical grade EP42HT-2ND2MED (Black) offers high temperature resistance and high strength for bonding, sealing, and coating applications. This non-drip adhesive features outstanding electrical insulative properties. Read more about Master Bond’s medical adhesives at http://www.masterbond.com/lp/tabs/tp_ind_medical.html or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #