This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=ms151.

----------------------------------

FOR IMMEDIATE RELEASE

New Flexible Low Viscosity 
Silicone Compound

HACKENSACK, NJ - Aug 30, 2007 -- MasterSil 151 is a new two component, low viscosity silicone compound for high performance casting, potting and encapsulation introduced by Master Bond Inc., Hackensack, N.J.  This formulation is designed to cure at room temperature or more rapidly at elevated temperatures.  MasterSil 151 has superior electrical insulation properties, high tensile strength and superb optical clarity.  It has a service operating temperature range of -65°F to +400°F.

MasterSil 151 is tough and flexible.   It has an elongation at break of 160% and a Shore A hardness of 45.  It has superior resistance to vibration, impact and shock.  It also is resistant to thermal cycling.  MasterSil 151 has a dielectric strength of 460 volts/mil and a volume resistivity of 1x1015 ohm cm.

Master Bond MasterSil 151 has a 10 to 1 mix ratio by weight.  Its low viscosity assures complete fill-in around complicated contours in even very complicated configurations.  Shrinkage upon cure is very low.  Shelf life in original containers is 6 months at 75°F.  MasterSil 151 is available for use in half- pint, pint, quart, gallon and 5 gallon kit containers.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #