This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=su10aoht-lo.

----------------------------------

FOR IMMEDIATE RELEASE

One Part High Strength Epoxy With
High Thermal Conductivity
Meets NASA Low Outgassing Specifications

HACKENSACK, NJ – June 8, 2010 – Resistance to impact, thermal shock, vibration and stress fatigue cracking is of vital importance in the aerospace, optical, medical and oil/chemical processing industries.  Master Bond Polymer Adhesive Supreme 10AOHT-LO is a single component, no mix, thermally conductive compound featuring superior electrical insulation and toughness.

It meets NASA low outgassing specifications and has superior durability and dimensional stability.  It is formulated to cure at elevated temperatures between 250°F and 300°F for 1 hour, and produces exceptional bonds for service over the wide temperature range of 4K to 400° F.  These tough bonds are remarkably resistant to severe thermal cycling and many chemicals, including water, oil and various fuels.

The hardened adhesive is a superb thermal conductor with a thermal conductivity of 9-10 BTU /in/ft²/hour/°F.  Its Shore D hardness exceeds 75 and its compressive strength is greater than 15,000 psi.  It is available for purchase in half pints, pints, quarts, gallons and 5 gallon containers.

Master Bond Low Outgassing Epoxies

Master Bond’s Supreme 10AOHT-LO is a NASA low outgassing, cryogenically serviceable, one part epoxy system formulated to stand up to impact, thermal shock, vibration and stress fatigue cracking.  Read more about Master Bond’s low outgassing epoxy formulations at http://www.masterbond.com/lp/tabs/tp_pp_lowoutgas.html, or contact Master Bond’s Technical Support Team by phone at +1-201-343-8983, by fax at +1-201-343-2132 or by e-mail at techinfo@masterbond.com.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #