Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.  This email was sent to (%email%)

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/newsrelease/uv15.

----------------------------------

FOR IMMEDIATE RELEASE

Dimensionally Stable Epoxy Based UV Curable System with High Temperature Resistance

HACKENSACK, NJ – August 16, 2012 – With its outstanding light transmission properties and optical clarity, Master Bond UV15 is widely used for a variety of bonding, coating and sealing applications in the optical, electronic and optoelectronic industries. This epoxy based UV curable system is 100% reactive and does not contain any solvents or other volatiles. It is also completely free of any oxygen inhibition.

Like most UV systems, Master Bond UV15 will cure quickly and easily when exposed to a UV light source with a wavelength range between 320-365 nm. It typically cures in thicknesses of a few microns to 0.015-0.020 inches in 15-30 seconds or less. UV15 cures by a cationic reaction and produces bonds that have lower shrinkage (1-2%) and higher temperature resistance than most UV systems. Its glass transition temperature (Tg) is 90-95°C with a straight UV cure. When post cured for 30 minutes at 125°C, the Tg is 125-130°C. The service temperature range for this system is -80°F to +350°F.

UV15 has excellent resistance to a wide variety of chemicals including water, acids, bases, fuels and many solvents. It features superb physical strength characteristics and electrical insulation properties. UV15’s low viscosity allows it to be spin coated. It has superior adhesion to a wide variety of substrates including plastics, glass and many metals. UV15 is available in syringes, ½ pints, pints, quarts, gallons and 5 gallon containers.

- Master Bond Electrically Insulative Adhesives

Featuring high dielectric strength, low dielectric constants and high volume resistivity Master Bond UV15 offers superior electrical insulation properties. Read more about Master Bond’s electrically insulative epoxies at http://www.masterbond.com/properties/electrically-insulative-adhesive-systems or contact Tech Support. Phone: +1-201-343-8983 Fax: +1-201-343-2132 Email: technical@masterbond.com.

Watch our video on UV15
http://youtu.be/LJoGPheDvdo

Check out more videos on our YouTube channel:

http://www.youtube.com/user/MasterBondVideo

Note to Editors:

Embed our video on UV15 right your website using the following code:

<iframe width="560" height="315" src="http://www.youtube.com/embed/LJoGPheDvdo" frameborder="0" allowfullscreen></iframe>

- CONTACT:

- James Brenner, Marketing Manager

- Email: jbrenner@masterbond.com

- Tel: +1-201-343-8983

Fax: +1-201-343-2132

- MASTER BOND INC.

- 154 Hobart Street

Hackensack, NJ 07601-3922

- Web: www.masterbond.com

# # #