This email was sent to (%email%)

Unsubscribe at: http://www.masterbond.com/phplist/?p=unsubscribe&id=2

Subscribe at: http://www.masterbond.com/phplist/?p=subscribe&id=2

----------------------------------

The following is a news release from Master Bond Inc.  You have received it because you are listed as an editor for your publication.

Attached to this email is a low resolution version of the photograph that is included in the press kit for this product.

High resolution versions of this image and files with the body text of this release are available at http://www.masterbond.com/mbnr.html?nr=uv15dc80.

----------------------------------

FOR IMMEDIATE RELEASE

New One Part UV and Heat 
Curable Epoxy System

HACKENSACK, NJ - Sep 28, 2006 -- Master Bond Inc., Hackensack, N.J. is pleased to announce the development of a special dual cure (UV/heat curable) epoxy system called UV15DC80.  It is designed for bonding, sealing, coating and potting applications.  This compound has a low viscosity, is easy to apply and requires no mixing.   Environmentally friendly, it is 100% solid and contains no solvents or volatiles.  UV15DC80 is not inhibited by oxygen and has low shrinkage upon cure.

Particularly noteworthy is that UV15DC80 can cure in shadowed areas by supplemental heat curing at 80C for 15-30 minutes.  Straight UV curing can be accomplished for thicknesses of .010”/.020” in seconds using UV light at 365 nm with 30-40 milliwatts per cm² of energy.  Faster cures can be achieved at higher energy outputs.  Post curing at 125-135C for 15-30 minutes can increase the Tg from 90C achieved by straight UV cure to over 130C.

UV15DC80 has high physical strength properties.  Adhesion to metals, glass, ceramics and most plastics is excellent.  It has superior chemical resistance.  Shore D hardness is >70 and its elongation after cure is 3-4%.  UV15DC80 has a tensile strength of >4,200 psi and a tensile modulus of 120,000 psi.  Its refractive index is 1.517.

Storage stability of UV15DC80 is 6 months at room temperature in the original unopened containers.  It is available for use in half-pint, pint, quart, gallon, and 5 gallon pail containers.  For ease of use, it also is available in syringe applicators.

CONTACT:

James Brenner, Marketing Manager

Email: jbrenner@masterbond.com

Tel: 201-343-8983

Fax: 201-343-2132

MASTER BOND INC.

154 Hobart Street

Hackensack, NJ  07601-3922

Web: www.masterbond.com

# # #